Table 1 - Mean visual rating, Mean mass losses, Mean percent mass loss and Mean percent termite mortality of bamboo blocks exposed to Coptotermes formosanus for 4 weeks in a no-choice laboratory test. Wood blocks visually rated using AWPA Standard - 2009 rating system; 10 (sound), 9.5 (trace, surface nibbles permitted), 9 (slight attack up to 3% of cross sectional area affected), 8 (moderate attack, 3-10 % of cross sectional area affected), 7 (moderate/severe attack, penetration, 10-30% of cross sectional area affected), 6 (severe attack,30-50% of cross sectional area affected), 4 (very severe attack, 50-70% of cross sectional area affected) or 0 (failure).

| Bamboo Species | Mean Visual Rating | Mean Mass Loss (g) | Mean Percent Mass loss (%) | Mean Percent Termite Mortality (%) |
| --- | --- | --- | --- | --- |
| Guadua angustifolia (GA) | 5.20 (±1.10) | 0.6912 (±0.1066) a | 24.77 (±2.12) | 18.90 (±5.67)cd |
| Bambusa hirose (BH) | 6.00 (±1.41) | 0.6214 (±0.0689) aa | 22.98 (±4.11) | 24.90 (±3.34)abc |
| Dendrocalamus latiflorus (DL) | 7.00 (±0.0000) | 0.5744 (±0.0546)ab | 22.56 (±2.63) | 25.40 (±6.55)bd |
| Dendrocalamus brandisii (DB) | 6.00 (±0.00) | 0.5227 (±0.0661)ab | 19.68 (±3.95) | 30.10 (±12.53)bd |
| Bambusa oldhamii (BO) | 6.40 (±0.55) | 0.4838 (±0.0663)b | 16.76 (±4.16) | 38.10 (±6.54)b |
| Gigantochola pseudoarundinacea (GP) | 7.40 (±0.55) | 0.4300 (±0.0265)b | 14.20 (±0.952) | 32.30 (±5.03)bd |

a Values in parentheses are standard deviations; means within a column followed by the same capital letter do differ significantly at the 5 percent level (ANOVA,Tukey’s HSD).

Mass losses of control woods were as follows: Bambusa hirose (BH) = 5.840% (±1.252), Bambusa oldhamii (BO) =5.253% (±0.734), Dendrocalamus brandisii (DB) = 8.123% (±0.891), Dendrocalamus latiflorus (DL) = 5.213% (±0.363), Gigantochola pseudoarundinacea (GP) = 2.620% (±0.865) and Guadua angustifolia (GA) = 4.960% (±0.355).

Table 2 - Mean visual rating, Mean mass losses, Mean percent mass loss and Mean termite mortality of bamboo blocks exposed to Coptotermes gestroi for 4 weeks in a no-choice laboratory test. Wood blocks visually rated using AWPA Standard - 2009 rating system; 10 (sound), 9.5 (trace, surface nibbles permitted), 9 (slight attack up to 3% of cross sectional area affected), 8 (moderate attack, 3-10 % of cross sectional area affected), 7 (moderate/severe attack, penetration, 10-30% of cross sectional area affected), 6 (severe attack,30-50% of cross sectional area affected), 4 (very severe attack, 50-70% of cross sectional area affected) or 0 (failure).

| Bamboo Species | Mean Visual Rating | Mean Mass Loss (g) | Mean Percent Mass loss (%) | Mean Percent Termite Mortality (%) |
| --- | --- | --- | --- | --- |
| Guadua angustifolia (GA) | 5.20 (±1.10) | 0.6514 (±0.0399)a | 29.14 (±3.28) | 18.90 (±3.52)d |
| Bambusa hirose (BH) | 6.00 (±1.41) | 0.5700 (±0.1009)aba | 26.94 (±8.02) | 41.00 (±13.98)abc |
| Dendrocalamus latiflorus (DL) | 6.00 (±0.00) | 0.6068 (±0.0602)a | 26.69 (±2.64) | 28.10 (±5.79)acd |
| Dendrocalamus brandisii (DB) | 7.00 (±0.00) | 0.4665 (±0.0136)bd | 22.10 (±2.23) | 27.60 (±2.79)acd |
| Bambusa oldhamii (BO) | 6.40 (±0.55) | 0.4526 (±0.0980)bc | 19.09 (±2.87) | 49.60 (±9.83)b |
| Gigantochola pseudoarundinacea (GP) | 7.40 (±0.55) | 0.3928 (±0.0284)cd | 14.51 (±1.241) | 41.50 (±9.07)abc |

a Values in parentheses are standard deviations; means within a column followed by the same capital letter do differ significantly at the 5 percent level (ANOVA, Tukey’s HSD).

Mass losses of control woods were as follows: Bambusa hirose (BH) = 4.530% (±1.770), Bambusa oldhamii (BO) =7.360% (±4.510), Dendrocalamus brandisii (DB) = 6.370% (±0.996), Dendrocalamus latiflorus (DL) 5.833% (±0.424), Gigantochola pseudoarundinacea (GP) = 3.7033% (±0.0950) and Guadua angustifolia (GA) = 4.710% (±1.395).