## Slide 1: Synthesis and Physicochemical properties of Dimer Acid 2-EthelhexylEsters as Potential Bio-lubricant
Shehu Isah
STLE Presentation

## Slide 2: Outline
Introduction
Synthesis of Dimer Acid 2-EH Ester
Characterization: NMR, MS-MS, FTIR
Physical Properties: Density, Viscosity and Kinematic viscosity
Blending and Cold flow properties
Conclusion
Acknowledgement

## Slide 3: Introduction
Derived from C36-Dimer acid, which were in turn a polymerized product of Oleic acid
Typically dicarboxylic acids from thermal polymerization of fatty acids
Commercially available from lower end as Azelaic acid (C9), Sebacic (C10), Undecanoic acid (C11) and C18 unsaturated fatty acids
C36 dimer acid

## Slide 4: Introduction
Applications of Dimer acids/esters
synthesis and production of polyamide,
lubricants hydraulic fluid, transmission oils and greases,
surface acting agent, corrosion inhibitors,
polyurethane resins or
cold flow improver (CFI) additives (Yasi et al., 2017).

## Slide 5: Synthesis of Dimer Acid 2-EH Ester
Optimized Large-scale Batch Process
synthesized from concentrated sulfuric acid catalyzed esterification C38 dimer acid at a ratio of 1:20 excess alcohol
The mixture was heated to 120 OC for 72 h and neutralized with 1.2 eq KOH in 90% ethanol /water
Excess 2-ethylhexanol via molecular distillation (wiped film evaporation)
Yield: 97 %

## Slide 6: Synthesis of Dimer Acid 2-EH Ester
Molecular Distillation
Evaporator Temp: 105 OC
Feed funnel Temp: 60 OC
Condenser Tender: 25 OC
Vacuum: 0.937 mmHg
Drop Rate: 20 drops/min.

## Slide 7: Synthesis of Dimer Acid 2-EH Ester
Application of Dean Stark Apparatus/Toluene
Dimer acid : 2-Ethyl hexanol (1:2.2 mol ratio)
Toluene (solvent)
H2SO4 (30% mole ratio of dimer acid)
Reflux under Nitrogen atm @ 140 OC for 48 h
Extracted with ethyl acetate
Yield 96.7 %

## Slide 8: Synthesis of Dimer Acid 2-EH Ester
Use of enclosed vial reactor without solvent
vial bottle lined with a teflon-lined capping
Dimer acid : 2-Ethyl hexanol (1:20 mol ratio)
H2SO4 (30% mole ratio of dimer acid)
Flush with Nitrogen @ 120 OC for 48 h
Extracted with ethyl acetate
Yield 97 %

## Slide 9: Characterization
13C NMR
Structural identification and
Monitor rate of conversion

## Slide 10: Characterization
MS-MS
Determination of molecular mass: m/z = 783.7g mol-1

## Slide 11: Characterization
MS-MS: Fragmentaion

## Slide 12: Characterization
FTIR

## Slide 13: Physical properties
Solubilities in Base Oils
Excellent solubility in both base oils: HOSuO and PAO-6

## Slide 14: Physical Properties
Total acid number
Total acid number decreased from ~ 180 to ~ 5 upon esterification
% FFA was approximately 3 % upon esterification
Dimer acid ET ester
Dimer acid
Microscale using Dean stark trap 184 | 5.55 (2.8) % FFA
Large scale batch 1 180 | 7.08 (3.57) %FFA
Large scale Batch 2 183 | 6.09 (3.55) % FFA

## Slide 15: Physical properties
Relative to oleic acid, dimer 2-EH esters displayed:
  Higher density (Batch-1 > Batch-2)
  3- to 8-fold higher kinematic viscosity (Batch-1 > Batch-2)
  Lower VI, which was comparable to PAO-6 ~ 137 (Batch-1 > Batch-2)
 | Fatty Acid |  | Dimer Ester | 
 | iso-Oleic | Oleic | Batch-1 | Batch-2
density, g/mL |  |  |  | 
40 °C | 0.8818 ± 0.0001 | 0.8777 ± 0.0001 | 0.9102 ± 0.0002 | 0.9128 ± 0.0001
100 °C | 0.8410 ± 0.0001 | 0.8368 ± 0.0000 | 0.8717 ± 0.0001 | 0.8739 ± 0.0000
kVis, mm2/s |  |  |  | 
40 °C | 28.01 ± 0.10 | 19.61 ± 0.01 | 161.79 ± 0.10 | 148.50 ± 0.14
100 °C | 5.82 ± 0.03 | 4.91 ± 0.01 | 19.10 ± 0.02 | 17.66 ± 0.01
dVis, mPa-s |  |  |  | 
40 °C | 24.70 ± 0.08 | 17.21 ± 0.01 | 147.26 ± 0.07 | 135.56 ± 0.14
100 °C | 4.89 ± 0.03 | 4.11 ± 0.01 | 16.65 ± 0.01 | 15.44 ± 0.01
VI | 158 ± 1 | 189± 0 | 134± 0 | 131. ± 0

## Slide 16: Physical properties
Density (g/cm3) of Dimer Ester blends in PAO-6
Neat PAO-6 has poor viscosity and VI properties
Blends with 0-10 % w/w dimer 2-EH esters were investigated:
  Higher density that increased with increasing [2-EH ester]

## Slide 17: Physical properties
Neat PAO-6 has poor viscosity and VI properties
Blends with 0-10 % w/w dimer 2-EH esters were investigated:
  Slight increase or no change in Kvis with increasing [2-EH ester]

## Slide 18: Physical properties
Neat PAO-6 has poor viscosity and VI properties
Blends with 0-10 % w/w dimer 2-EH esters were investigated:
  Slight increase or no change in VI with increasing [2-EH ester]

## Slide 19: Cold Flow properties
Neat HOSuO has poor cold flow
Blends with 0-10 % w/w dimer esters investigated
  Lower pour point that was independent of [2-EH ester]
  Slight reduction in cloud point that decreased with increasing [2-EH ester]
Pour Point and Cloud Point of Dimer Ester-2 blends in HOSuO

## Slide 20: Physical properties: Oxidation Stability
PDSC onset (OT) and peak (PT) oxidation temperatures of Dimer Ester-1 blends in HOSuO (°C)
Slight reduction in oxidation OT and PT that was independent of [2-EH ester

## Slide 21: Physical Properties
Findings
Good solubility profiles in commercial base oils: > 20 % (w/w)
Kinematic viscosity and viscosity index compared favorably well with commercial base oil (PAO-6): 134 v 137
Improved CP, PP, density and kinematic viscosity upon blending with commercial base stock
Potential for bio lubricant formulation or
Candidate for CFI additive

## Slide 22: Conclusion
Dimer acid 2-EH esters were synthesized from sulfuric acid catalyzed esterification of C36 dimer acid with 2-ethylhexanol
Reaction parameters optimized for scale up production of two batches of dimer esters obtained from two set of dimer acids catalyzed by different zeolite catalysts.
Reaction progress and conversion were monitored 13C NMR spectroscopy.
Dimer acid 2-EH esters compared favorably well with commercial base oil (PAO-6) as potential candidate for base stock formulation.
Blends of dimer acid 2EH ester with HOSuO base stock showed improvement in cloud point and pour point as potential cold flow property improver (CFI) additive.
The OT and PT oxidative temperatures were slightly lower than the HOSuO base stocks.